**Product Description**

NovaBond SignFix XS 100C is a clear acrylic tape with a red double sided siliconised filmic liner. The product utilises the latest high strength, solvent free technology to satisfy the demanding criteria of the signmaker and other industries requiring critical, consistent and reliable performance whilst being friendly to the environment. The water clear appearance of the product makes it ideal where aesthetics demand a colourless bond line.

**Product Specification**

Colour – Clear

Carrier – Acrylic

Liner – Red PE

Thickness – 1mm ( ± 10% )

Length – 33m

Standard Roll Dimensions – 12, 19, 25mm

Logs – 930mm

**Product Benefits**

* High tack and initial bond strength improving process efficiency
* Water clear appearance giving an invisible bond line where aesthetics demand.
* Easy release double sided siliconised filmic liner to speed up assembly
* Incredibly high bond strength for peace of mind
* Withstands extremes of temperature, water, most solvents and chemicals, differential expansion and contraction and high forces applied to the bond providing superior durability, longevity and exterior performance
* Please refer to Bonding To Glass Procedure document and use in conjunction with NovaBond Gllass Primer for best results on glass.

**Best Practice**

Where possible, and aesthetics allow, always abrade the surface to provide a ‘ key ‘.  This can increase the ultimate bond strength by as much as 35%.  Clean with NovaBond Surface Cleaner and prime with the relevant NovaBond Surface Primer.  Independent tests at Loughborough University have shown the correct primer to increase the ultimate bond strength by up to 50%.

**Product Data**

|  |  |
| --- | --- |
| Dynamic Shear\*  ( Mean Load ) | 362N ( Surface area 800mm² )  Force Applied 45N for 60 seconds  Jaw Speed 10mm/minute |
| 180° Peel\*  ( Mean Load ) | 33N ( Surface Area 60mm² )  Force Applied 20N  Jaw Speed 50mm/minute |
| Tensile Load\*  ( Mean Load ) | 68N ( Surface Area 122mm² )  Force Applied 45N for 60 seconds  Jaw Speed 10mm/minute |

|  |
| --- |
| Data taken from independent testing commissioned at Joint Testing Services by Dr. Paul Briskham |

|  |  |
| --- | --- |
| Service Temperature | -40°C - 120°C  Short Term 150°C |
| Elongation | >700% |
| Application Temperature | Minimum 15°C  (ideally between 21°c and 40°C )  Relative Humidity 55% ± 10% |

For any other advice or on-site consultation, please contact us via our details below or go to our online demonstration video at: - <http://bit.ly/novabond>

[**http://www.innovasolutionsonline.co.uk/**](http://www.innovasolutionsonline.co.uk/)

**Innova-Strapline-250.png**

**Lower Draught Gates Farm,**

**Burnley Road,**

**Trawden,**

**Lancashire**

**BB8 8PW**

**Tel: 01282 867390**

**Fax: 01282 861077**

**E-mail:** [**info@innovasolutionsonline.com**](mailto:info@innovasolutionsonline.com)

Disclaimer

The information contained herein is produced in good faith and is believed to be reliable but is for guidance only. Innova Solutions Ltd and its agents cannot assume liability or responsibility for results obtained in the use of its products by persons whose methods are outside or beyond our control. It is the users’ responsibility to determine the suitability of any of the products and methods of use or preparation prior to use mentioned in out literature and furthermore the users’ responsibility to observe and adopt such precautions as may be advisable for the protection of personnel and property in the handling and use of any of our products.